## Slide 1: Fourier Synthesis Illuminator for EUV mask inspection tool
Markus P. Benk, Kenneth A. Goldberg, Iacopo Mochi, Patrick P. Naulleau
SRI2013, Gaithersburg MD, June 20

## Slide 3: Outline
Introduction
  SHARP microscope
Fourier Synthesis Illuminator
  Concept
  Layout
  Components
  Pupil-fill
  Uniformity
Images
  Effect of illumination on imaging
Summary

## Slide 4: Mask inspection
Sematech High-NA Actinic Reticle Review Project
SEM image
Defect on
EUV photolithography mask
Mochi, SPIE 7636 (2009)
SHARP

## Slide 5: Mask inspection
Sematech High-NA Actinic Reticle Review Project
Mochi, SPIE 7636 (2009)
SEM image EUV image
SHARP

## Slide 6: Mask inspection
Sematech High-NA Actinic Reticle Review Project
In-focus image
Goldberg, SPIE 8679 (2013)
Defect on
EUV photolithography mask
EUV image
SHARP

## Slide 7: Mask inspection
Sematech High-NA Actinic Reticle Review Project
In-focus image Out-of-focus image
Goldberg, SPIE 8679 (2013)
SHARP

## Slide 8: Layout
PHOTOMASK
LENS
ILLUMINATOR
CCD
SHARP

## Slide 9: Zoneplates
Tool performance
  5 s Exposure time
  8 Defect locations per hour
  (160 images)
Goldberg, SPIE 8679 (2013)
  200 zoneplates
  3 zoneplate chips
  5 Azimuthal angles
  0.0625 to 0.156 NA
  6° to 10° central ray angle
SHARP
160 µm
6 mm

## Slide 10: Spatial coherence
Condenser
Coherence area
Fourier Synthesis Illuminator

## Slide 11: Spatial coherence
Condenser
Coherence area
Fourier Synthesis Illuminator

## Slide 12: Spatial coherence
Spatial resolution
Lens
Fourier Synthesis Illuminator

## Slide 13: Spatial coherence
Spatial resolution
Lens
Fourier Synthesis Illuminator

## Slide 14: Spatial coherence
Fourier Synthesis Illuminator
NA Condenser
NA Lens

## Slide 15: Pupil fill
Zoneplate aperture
Fourier Synthesis Illuminator

## Slide 16: Pupil fill
s =0.25
Fourier Synthesis Illuminator

## Slide 17: Pupil fill
s =0.8
Fourier Synthesis Illuminator

## Slide 18: Pupil fill
Annular fill
Fourier Synthesis Illuminator

## Slide 19: Pupil fill
Dipole
Fourier Synthesis Illuminator

## Slide 20: Pupil fill
Crosspole
Fourier Synthesis Illuminator

## Slide 21: Layout
PHOTOMASK
LENS
ILLUMINATOR
CCD
Fourier Synthesis Illuminator

## Slide 22: Layout
ILLUMINATOR
Fourier Synthesis Illuminator

## Slide 23: Layout
4-jaw slits
Mb
Ma
Mc
Fourier Synthesis Illuminator

## Slide 24: Layout
Mb
Ma
Mc
Fourier Synthesis Illuminator

## Slide 25: Layout
Mb
Ma
Mc
Fourier Synthesis Illuminator

## Slide 26: Layout
Mb
Ma
Mc
Fourier Synthesis Illuminator

## Slide 27: Layout
Mb
Ma
Mc
Fourier Synthesis Illuminator

## Slide 28: Ma mirror
  1 mm dia. flat Si substrate
  1° range of incidence angles
  10 bi-layer Mo/Si coating
Mirrorcle
  gimbal-less dual-axis, scanning MEMS device
  2 kHz scan rate
Goldberg, SPIE 8679 (2013)
Fourier Synthesis Illuminator

## Slide 29: Mb mirror
  50 mm x 36 mm flat
  > 2° range of inc. angles
  40 Mo/Si bi-layers
Goldberg, SPIE 8679 (2013)
Fourier Synthesis Illuminator

## Slide 30: Mc mirror
  48 mm x 35 mm poly Si
  ellipsoidal surface
  10x demagnification
  42 Mo/Si bi-layers
  0.15 nm RMS roughness
  <25 µrad slope error
Actuator
  Piezo-driven dual-axis scanner
  200 Hz scan rate
  2 mrad scanning range
Goldberg, SPIE 8679 (2013)
Fourier Synthesis Illuminator

## Slide 31: Mc mirror
Coating
  15° range of incidence angles
Fourier Synthesis Illuminator

## Slide 32: Mc mirror
Coating
Goldberg, SPIE 8679 (2013)
Fourier Synthesis Illuminator

## Slide 33: Pupil fill monitor
  In-vacuum YAG camera
  2x magnification
  2.1 µm per pixel
Fourier Synthesis Illuminator

## Slide 34: Pupil fill monitor
  In-vacuum YAG camera
  2x magnification
  2.1 µm per pixel
Fourier Synthesis Illuminator

## Slide 35: Pupil fill monitor
  In-vacuum YAG camera
  2x magnification
  2.1 µm per pixel
Fourier Synthesis Illuminator

## Slide 36: Pupil fill
Lissajous pattern on Mc mirror
Fourier Synthesis Illuminator

## Slide 37: Pupil fill
Lissajous pattern on Mc mirror
Fourier Synthesis Illuminator

## Slide 38: Pupil fill
static beam
Fourier Synthesis Illuminator

## Slide 39: Pupil fill
0.156 NA 10° CRA s=0.8
Fourier Synthesis Illuminator

## Slide 40: Pupil fill
0.156 NA 10° CRA s=0.8 -25° azimuth
Fourier Synthesis Illuminator

## Slide 41: Pupil fill
0.156 NA 10° CRA s=0.8 +25° azimuth
Fourier Synthesis Illuminator

## Slide 42: Pupil fill
0.125 NA 8° CRA s1=0.2 s2=0.8
Fourier Synthesis Illuminator

## Slide 43: Pupil fill
Dipole 0.125 NA 8° CRA
Fourier Synthesis Illuminator

## Slide 44: Pupil fill
Quadrupole 0.125 NA 8° CRA
Fourier Synthesis Illuminator

## Slide 45: Pupil fill
Quadrupole 45° 0.125 NA 8° CRA
Fourier Synthesis Illuminator

## Slide 46: Pupil fill
Crosspole 0.125 NA 8° CRA
Fourier Synthesis Illuminator

## Slide 47: Uniformity
No Mc scanning
Fourier Synthesis Illuminator
5 µm
Image of mask blank surface s=0.55 900x mag

## Slide 48: Uniformity
Raster 8 lines 2 µm x 2 µm
Fourier Synthesis Illuminator

## Slide 49: Uniformity
Raster 8 lines 4 µm x 4 µm
Fourier Synthesis Illuminator

## Slide 50: Uniformity
Raster 8 lines 6 µm x 6 µm
Fourier Synthesis Illuminator

## Slide 51: Uniformity
Raster 8 lines 8 µm x 8 µm
Fourier Synthesis Illuminator

## Slide 52: Uniformity
Raster 8 lines 10 µm x 10 µm
Fourier Synthesis Illuminator

## Slide 53: Uniformity
Raster 8 lines 12 µm x 12 µm
Fourier Synthesis Illuminator

## Slide 54: Uniformity
10% Uniformity region through-focus series
2% Uniformity region single image
Fourier Synthesis Illuminator

## Slide 55: Modulation in the Image
Images
Attwood, Soft x-rays and extreme ultraviolet radiation, Cambridge University Press (1999)

## Slide 56: Through-focus
0.0625 NA 125 nm lines and spaces
s =1
s ≈ 0
Images

## Slide 57: Through-focus
0.0625 NA 125 nm lines and spaces
s =1
s ≈ 0
Images

## Slide 58: Through-focus
0.0625 NA 125 nm lines and spaces
s =1
s ≈ 0
Images

## Slide 59: Through-focus
0.0625 NA 125 nm lines and spaces
s =1
s ≈ 0
Images

## Slide 60: Through-focus
0.0625 NA 125 nm lines and spaces
s =1
s ≈ 0
Images

## Slide 61: Through-focus
s =1
s ≈ 0
Images
0.0625 NA 125 nm lines and spaces

## Slide 62: Through-focus
s =1
s ≈ 0
Images
0.0625 NA 125 nm lines and spaces

## Slide 63: Through-focus
0.0625 NA 125 nm lines and spaces
s =1
s ≈ 0
Images

## Slide 64: Through-focus
Images
Vertical lines

## Slide 65: In-focus
0.0625 NA 100 nm lines and spaces
s =1
Images

## Slide 66: In-focus
0.0625 NA 100 nm lines and spaces
s =1
Images

## Slide 67: In-focus
0.0625 NA 100 nm lines and spaces
s =0.5
Images

## Slide 68: In-focus
0.0625 NA 100 nm lines and spaces
Images
s =0.25

## Slide 69: In-focus
0.0625 NA 100 nm lines and spaces
s =0.05
Images

## Slide 70: In-focus
Images
incoherent
coherent
Horizontal lines

## Slide 71: Directional pupil fill
0.0625 NA 100 nm lines and spaces
Vertical dipole
Images

## Slide 72: Directional pupil fill
0.0625 NA 100 nm lines and spaces
Vertical dipole
Images

## Slide 73: Directional pupil fill
0.0625 NA 100 nm lines and spaces
Images
Vertical dipole

## Slide 74: Directional pupil fill
0.0625 NA 100 nm lines and spaces
Images
Vertical dipole

## Slide 75: Directional pupil fill
0.0625 NA 100 nm lines and spaces
Images
Vertical dipole

## Slide 76: Directional pupil fill
0.0625 NA 100 nm lines and spaces
Images
Vertical dipole

## Slide 77: Directional pupil fill
0.0625 NA 100 nm lines and spaces
Images
Vertical dipole

## Slide 78: Directional pupil fill
0.0625 NA 100 nm lines and spaces
Images
Vertical dipole

## Slide 79: Directional coherence
Images
Horizontal lines

## Slide 80: Summary
Sematech High-NA Actinic Reticle Review Project
  EUV mask and pattern inspection tool
Fourier Synthesis Illuminator
  Lossless control of spatial coherence and pupil fill
  Scanner for uniformity control
Imaging
  Influence of spatial coherence on contrast, resolution and depth-of-field
  Directional pupil fill

## Slide 81: Summary
Acknowledgement
  This work was funded by SEMATECH through the U.S. Department of Energy under Contract No. DE-AC02-05CH11231
Thank you!